## Slide 1
7.2.1 Grades of Steel
Structural steel grades are referred to by their corresponding ASTM designation. For example, the most commonly used grade of structural steel is A36, which is produced to meet the requirements of the ASTM A36 specification.
This grade offers a good mix of strength, weldability, and cost. In many designs, this specification alone will satisfy designers’ needs. Other specifications, such as A53 for pipe, provide an equivalent grade of steel for that type of product. However, as loads on the structural elements becomes larger, other grades of steel may become more economical because of dimensional limitations or simpler fabrication. These grades provide greater strength levels at somewhat higher costs per unit weight.
ASTM specification | Thickness, in | Minimum tensile strength, ksi | Minimum yield stress,* ksi
A36 A529 | To 8 in incl. To 1⁄2 in incl. | 58–80† 60–85† | 36 42
A441 A572 A242 A588 A992 | To 3⁄4 incl. Over 3⁄4 to 11⁄2 Over 11⁄2 to 4 incl. Over 4 to 8 incl. Gr 42: to 4 incl. Gr 45: to 11⁄2 incl. Gr 50: to 11⁄2 incl. Gr 55: to 11⁄2 incl. Gr 60: to 1 incl. Gr 65: to 1⁄2 incl. To 3⁄4 incl. Over 3⁄4 to 11⁄2 Over 11⁄2 to 4 incl. To 4 incl. Over 4 to 5 Over 5 to 8 incl. Shapes only | 70 67 63 60 60 60 65 70 75 80 70 67 63 70 67 63 65 | 50 46 42 40 42 45 50 55 60 65 50 46 42 50 46 42 50
A514 | To 3⁄4 incl. | 115–135 | 100
 | Over 3⁄4 to 21⁄2 | 115–135 | 100
 | Over 21⁄2 to 4 incl. | 105–135 | 90
TABLE 7.2 Characteristics of Structural Steels
Carbon Steels
High-strength, low-alloy steels
Heat-treated low-alloy steels